G-NOR ELECTRONICS CO.,LTD.

| GNL-3014xx (Φ3mm ROUND TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter; Unit. DC Forward Current; 30; mA. Reverse Voltage; 5; V. Reverse Current (Vr-5V); 10; µA. Peak Forward Current ,tw ,=1 msec Duty ,=1/20; 150; mA. Operation Temperature; -40; +80; ℃. Storage Temperature; -40; +100; ℃. Solder Dip (5 seconds,1.6mm from body ) Temperature; 300; ±5; ℃. |  |
| --- | --- |
| Part Number; EMITTED COLOR; Lens Color; Peak Wavelength (nm); Vf (v) Typ.; IV (If=20mA) mcd; View Angle 2θ1/2. Min.; Typ.. GNL-3014SRD; GaAlAs; Super Red; Red Diffused; 660; 1.9; 70; 100; 60°. GNL-3014SRT; GaAlAs; Super Red; Red Transparent; 660; 1.9; 150; 200; 25°. GNL-3014SRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 150; 200; 25°. GNL-3014LRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 200; 300; 25°. GNL-3014URC; GaAlAs; Super Red; Water Clear; 660; 1.9; 500; 600; 25°. GNL-3014UEC; AlGaInP; Super Orange; Water Clear; 625; 2.0; 1000; 1500; 25°. GNL-3014HRC; AlGaInP; Super Orange; Water Clear; 640; 2.0; 500; 800; 25°. GNL-3014HRT; AlGaInP; Super Orange; Red Transparent; 640; 2.0; 500; 800; 25°. GNL-3014HRD; AlGaInP; Super Orange; Red Diffused; 640; 2.0; 150; 300; 60°. GNL-3014UGC; AlGaInP; Yellow Green; Water Clear; 572; 2.0; 350; 500; 25°. GNL-3014GC; GaP; Green; Water Clear; 565; 2.0; 30; 40; 25°. GNL-3014YC; GaAsP; Yellow; Water Clear; 588; 2.0; 30; 40; 25°. GNL-3014UYC; AlGaInP; Super Yellow; Water Clear; 589; 2.0; 800; 1000; 25°. GNL-3014BC; InGaN; Super Blue; Water Clear; 470; 3.5; 1000; 1500; 25°. GNL-3014UBC; InGaN; Ultra Super Blue; Water Clear; 470; 3.5; 1200; 2000; 25°. GNL-3014BGC; InGaN; Super Bluish Green; Water Clear; 505; 3.5; 2500; 4000; 25°. GNL-3014PGC; InGaN; Super Pure Green; Water Clear; 525; 3.5; 2500; 4000; 25°. GNL-3014UWC; InGaN; Ultra Super White; Water Clear; 5500K-7000K; 3.5; 2000; 3000; 25°. GNL-3014VC; InGaN; Super Violet; Water Clear; 400; 3.5; 150; 300; 25°. |