G-NOR ELECTRONICS CO.,LTD.

| GNL-5013xx (Φ5mm ROUND TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter; Unit. DC Forward Current; 30; mA. Reverse Voltage; 5; V. Reverse Current (Vr-5V); 10; µA. Peak Forward Current ,tw ,=1 msec Duty ,=1/20; 150; mA. Operation Temperature; -40; +80; ℃. Storage Temperature; -40; +100; ℃. Solder Dip (3 seconds,1.6mm from body ) Temperature; 260; ±5; ℃. |  |
| --- | --- |
| Part Number; EMITTED COLOR; Lens Color; Peak Wavelength (nm); Vf (v) Typ.; IV (If=20mA) mcd; View Angle 2θ1/2. Min.; Typ.. GNL-5013SRD; GaAlAs; Super Red; Red Diffused; 660; 1.9; 50; 100; 60°. GNL-5013SRT; GaAlAs; Super Red; Red Transparent; 660; 1.9; 250; 400; 18°. GNL-5013SRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 250; 400; 18°. GNL-5013LRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 400; 500; 18°. GNL-5013LRD; GaAlAs; Super Red; Red Diffused; 660; 1.9; 100; 150; 60°. GNL-5013URC; GaAlAs; Super Red; Water Clear; 660; 1.9; 600; 800; 18°. GNL-5013UEC; AlGaInP; Super Orange Red; Water Clear; 625; 2.0; 1200; 1500; 18°. GNL-5013HRC; AlGaInP; Super Orange Red; Water Clear; 640; 2.0; 500; 1000; 18°. GNL-5013HRD; AlGaInP; Super Orange Red; Red Diffused; 640; 2.0; 250; 500; 60°. GNL-5013GC; GaP; Green; Water Clear; 565; 2.0; 40; 50; 18°. GNL-5013UGC; AlGaInP; Yellow Green; Water Clear; 572; 2.0; 600; 800; 18°. GNL-5013UGD; AlGaInP; Yellow Green; Green Diffused; 572; 2.0; 150; 200; 60°. GNL-5013YC; GaAsP; Yellow; Water Clear; 588; 2.0; 40; 50; 18°. GNL-5013UYC; AlGaInP; Super Yellow; Water Clear; 590; 2.0; 1200; 1500; 18°. GNL-5013BC; InGaN; Super Blue; Water Clear; 470; 3.5; 1000; 1500; 18°. GNL-5013UBC; InGaN; Ultra Super Blue; Water Clear; 470; 3.5; 1500; 2000; 18°. GNL-5013UBW; InGaN; Ultra Super Blue; Milk Diffused; 470; 3.5; 800; 1500; 60°. GNL-5013BGC; InGaN; Super Bluish Green; Water Clear; 505; 3.5; 4000; 5000; 18°. GNL-5013PGC; InGaN; Super Pure Green; Water Clear; 525; 3.5; 5000; 7000; 18°. GNL-5013VC; InGaN; Super Violet; Water Clear; 395; 3.5; 50; 100; 18°. GNL-5013UVC; InGaN; Ultra Violet; Water Clear; 270; 6.0; 2MW; 3MW; 25°. GNL-5013UEC-1; AlGaInP; Super Orange Red; Water Clear; 625; 2.0; 1000; 1200; 18°. GNL-5013UYC-1; AlGaInP; Super Yellow; Water Clear; 590; 2.0; 1000; 1200; 18°. GNL-5013PGC-1; InGaN; Super Pure Green; Water Clear; 525; 3.5; 4000; 5000; 18°. |