G-NOR ELECTRONICS CO.,LTD.

| GNL-5033xx (Φ5mm Flat Top TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter; Unit. DC Forward Current; 30; mA. Reverse Voltage; 5; V. Reverse Current (Vr-5V); 10; µA. Peak Forward Current ,tw ,=1 msec Duty ,=1/20; 150; mA. Operation Temperature; -40; +80; ℃. Storage Temperature; -40; +100; ℃. Solder Dip (5 seconds,1.6mm from body ) Temperature; 300; ±5; ℃. |  |
| --- | --- |
| Feature: 1.Small flange without stand-off 2.Long life-solid state reliability 3.Long lead length(25.4mm) 4.Versatile mounting on P.C. board or panel Description: 1.The shape of this series is round 2.General application is for indication,illumination,etc. 3.These LED lamps are available with a choice of defferent colors,light intensities,epoxy colors,etc. |  |
| # Part Number; EMITTED COLOR; Lens Color; Peak Wavelength (nm); Vf (v) Typ.; IV (If=20mA) mcd; View Angle 2θ1/2. Min.; Typ.. GNL-5033URC; GaAlAs; Super Red; Water Clear; 660; 1.9; 110; 120; 90°. GNL-5033UEC; AlGaInP; Super Orange; Water Clear; 625; 2.0; 120; 130; 90°. GNL-5033HRC; AlGaInP; Super Orange; Water Clear; 640; 2.0; 60; 90; 90°. GNL-5033UGC; AlGaInP; Yellow Green; Water Clear; 572; 2.0; 50; 70; 90°. GNL-5033UYC; AlGaInP; Super Yellow; Water Clear; 588; 2.0; 120; 130; 90°. GNL-5033UBC; InGaN; Ultra Super Blue; Water Clear; 470; 3.5; 200; 250; 90°. GNL-5033PGC; InGaN; Super Pure Green; Water Clear; 525; 3.5; 550; 600; 90°. GNL-5033UEC-TL; AlGaInP; Super Orange; Water Clear; 625; 2.0; 300; 320; 90°. GNL-5033UYC-TL; AlGaInP; Super Yellow; Water Clear; 588; 2.0; 300; 320; 90°. GNL-5033UWC; InGaN; Super white; Water clear; 5500K-7000K; 3.5; 300; 500; 90°. |