G-NOR ELECTRONICS CO.,LTD.

| GNL-5073xx (Φ5mm ROUND TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter; Unit. DC Forward Current; 30; mA. Reverse Voltage; 5; V. Reverse Current (Vr-5V); 10; µA. Peak Forward Current ,tw ,=1 msec Duty ,=1/20; 150; mA. Operation Temperature; -40; +80; ℃. Storage Temperature; -40; +100; ℃. Solder Dip (5 seconds,1.6mm from body ) Temperature; 300; ±5; ℃. |  |
| --- | --- |
| Feature: Description: 1.Small flange without stand-off 1.The shape of this series is round 2.Long life-solid state reliability 2.General application is for indication,illumination,etc. 3.Long lead length(25.4mm) 3.These LED lamps are available with a choice of defferent 4.Versatile mounting on P.C. board or panel colors,light intensities,epoxy colors,etc. |  |
| # Part Number; EMITTED COLOR; Lens Color; Peak Wavelength (nm); Vf (v) Typ.; IV (If=20mA) mcd; View Angle 2θ1/2. Min.; Typ.. GNL-5073URC; GaAlAs; Super Red; Water Clear; 660; 1.9; 80; 150; 120°. GNL-5073UEC; AlGaInP; Super Red; Water Clear; 625; 2.0; 80; 150; 120°. GNL-5073HRC; AlGaInP; Super Red; Water Clear; 640; 2.0; 70; 120; 120°. GNL-5073UYC; AlGaInP; Super Yellow; Water Clear; 590; 2.0; 80; 150; 120°. GNL-5073UBC; InGaN; Super Blue; Water Clear; 470; 3.5; 90; 150; 120°. GNL-5073PGC; InGaN; Pure Green; Water Clear; 525; 3.5; 300; 400; 120°. GNL-5073BGC; InGaN; Super Cyan; Water Clear; 505; 3.5; 200; 300; 120°. GNL-5073UGC; AlGaInP; Yellow Green; Water Clear; 572; 2.0; 60; 100; 120°. GNL-5073UEC-TL; AlGaInP; Ultra Super Red; Water Clear; 625; 2.0; 150; 250; 120°. GNL-5073UYC-TL; AlGaInP; Ultra Super Yellow; Water Clear; 590; 2.0; 150; 250; 120°. GNL-5073UBC-TL; InGaN; Ultra Super Blue; Water Clear; 470; 3.5; 150; 250; 120°. GNL-5073PGC-TL; InGaN; Ultra Super Green; Water Clear; 525; 3.5; 400; 500; 120°. GNL-5073UWC; InGaN; Ultra Super White; Water Clear; 5500K-7000K; 3.5; 700; 800; 120°. GNL-5073UWC-Y; InGaN; Ultra Warm White; Water Clear; 2700K-3500K; 3.5; 500; 600; 120°. |