G-NOR ELECTRONICS CO.,LTD.

| GNL-10003xx (Φ10mm ROUND TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter; Unit. DC Forward Current; 30; mA. Reverse Voltage; 5; V. Reverse Current (Vr-5V); 10; µA. Peak Forward Current ,tw ,=1 msec Duty ,=1/20; 150; mA. Operation Temperature; -40; +80; ℃. Storage Temperature; -40; +100; ℃. Solder Dip (5 seconds,1.6mm from body ) Temperature; 300; ±5; ℃. |  |
| --- | --- |
| # Part Number; EMITTED COLOR; Lens Color; Peak Wavelength (nm); Vf (v) Typ.; IV (If=20mA) mcd; View Angle 2θ1/2. Min.; Typ.. GNL-10003SRD; GaAlAs; Super Red; Red Diffused; 660; 1.9; 50; 80; 60°. GNL-10003LRD; GaAlAs; Super Red; Red Diffused; 660; 1.9; 60; 100; 60°. GNL-10003SRT; GaAlAs; Super Red; Red Transparent; 660; 1.9; 250; 400; 22°. GNL-10003SRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 250; 400; 22°. GNL-10003LRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 200; 400; 22°. GNL-10003URC; GaAlAs; Super Red; Water Clear; 660; 1.9; 1000; 1500; 22°. GNL-10003UEC; AlGaInP; Super Orange; Water Clear; 625; 2.0; 1500; 2000; 22°. GNL-10003HRC; AlGaInP; Super Orange; Water Clear; 640; 2.0; 1000; 1500; 22°. GNL-10003GC; GaP; Green; Water Clear; 565; 2.0; 40; 50; 22°. GNL-10003UGC; AlGaInP; Yellow Green; Water Clear; 572; 2.0; 600; 800; 22°. GNL-10003YC; GaAsP; Yellow; Water Clear; 585; 2.0; 40; 50; 22°. GNL-10003UYC; AlGaInP; Super Yellow; Water Clear; 589; 2.0; 1200; 1800; 22°. GNL-10003BC; InGaN; Super Blue; Water Clear; 470; 3.5; 800; 1200; 22°. GNL-10003UBC; InGaN; Ultra Super Blue; Water Clear; 470; 3.5; 1000; 1800; 22°. GNL-10003BGC; InGaN; Super Bluish Green; Water Clear; 505; 3.5; 3000; 4000; 22°. GNL-10003PGC; InGaN; Super Pure Green; Water Clear; 525; 3.5; 3000; 5000; 22°. GNL-10003UWC; InGaN; Ultra Super White; Water Clear; 5500K-7000K; 3.5; 4000; 5500; 22°. GNL-10003VC; InGaN; Super Violet; Water Clear; 400; 3.5; 100; 300; 22°. |