G-NOR ELECTRONICS CO.,LTD.

| GNL-20003xx (Φ20mm ROUND TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) |  |  |  |  |  |  | 3 4 1 2 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Parameter |  |  |  |  |  | Unit |  |  |  |  |  |
| DC Forward Current |  |  | 30 |  |  | mA |  |  |  |  |  |
| Reverse Voltage |  |  | 5 |  |  | V |  |  |  |  |  |
| Reverse Current (Vr-5V) |  |  | 10 |  |  | µA |  |  |  |  |  |
| Peak Forward Current ,tw ,=1 msec Duty ,=1/20 |  |  | 150 |  |  | mA |  |  |  |  |  |
| Operation Temperature |  |  | -40 |  | +80 | ℃ |  |  |  |  |  |
| Storage Temperature |  |  | -40 |  | +100 | ℃ |  |  |  |  |  |
| Solder Dip (5 seconds,1.6mm from body ) Temperature |  |  | 260 |  | ±5 | ℃ |  |  |  |  |  |
| Feature: 1.Small flange without stand-off 2.Long life-solid state reliability 3.Versatile mounting on P.C. board or panel Description: - The shape of this series is round - General application is for indication,illumination,etc. 3.These LED lamps are available with a choice of defferent colors,light intensities,epoxy colors,etc. |  |  |  |  |  |  |  |  |  |  |  |
| Part Number | EMITTED COLOR |  |  | Lens Color |  |  | Peak Wavelength (nm) | Vf (v) Typ. | IV (If=20mA) mcd |  | View Angle 2θ1/2 |
|  |  |  |  |  |  |  |  |  | Min. | Typ. |  |
| GNL-20003SRD | GaAlAs | Super Red |  | Red Diffused |  |  | 660 | 1.9 | 75 | 150 | 120° |
| GNL-20003LRD | GaAlAs | Super Red |  | Red Diffused |  |  | 660 | 1.9 | 100 | 200 | 120° |
| GNL-20003UED | AlGaInP | Super Orange Red |  | Red Diffused |  |  | 625 | 2.0 | 200 | 400 | 120° |
| GNL-20003UGD | AlGaInP | Yellow Green |  | Green Diffused |  |  | 572 | 2.0 | 150 | 300 | 120° |
| GNL-20003UYD | AlGaInP | Super Yellow |  | Yellow Diffused |  |  | 588 | 2.0 | 200 | 400 | 120° |
| GNL-20003UBD | InGaN | Super Blue |  | Blue Diffused |  |  | 470 | 3.5 | 250 | 400 | 120° |
| GNL-20003PGD | InGaN | Super Pure Green |  | Green Diffused |  |  | 525 | 3.5 | 900 | 1200 | 120° |
| GNL-20003WW | InGaN | Super White |  | White Diffused |  |  |  | 3.5 | 1000 | 2000 | 120° |
| GNL-20003UWW | InGaN | Super White |  | White Diffused |  |  |  | 3.5 | 1800 | 3500 | 120° |
| GNL-20003SRT | GaAlAs | Super Red |  | Red Clear |  |  | 660 | 1.9 | 90 | 180 | 60° |
| GNL-20003LRT | GaAlAs | Super Red |  | Red Clear |  |  | 660 | 1.9 | 120 | 240 | 60° |
| GNL-20003UET | AlGaInP | Super Orange Red |  | Red Clear |  |  | 625 | 2.0 | 240 | 480 | 60° |
| GNL-20003UGT | AlGaInP | Yellow Green |  | Green Clear |  |  | 572 | 2.0 | 180 | 360 | 60° |
| GNL-20003UYT | AlGaInP | Super Yellow |  | Yellow Clear |  |  | 588 | 2.0 | 240 | 480 | 60° |
| GNL-20003UBT | InGaN | Super Blue |  | Blue Clear |  |  | 470 | 3.5 | 300 | 480 | 60° |
| GNL-20003PGT | InGaN | Super Pure Green |  | Green Clear |  |  | 525 | 3.5 | 1200 | 2000 | 60° |
| GNL-20003WC | InGaN | Super White |  | Water clear |  |  |  | 3.5 | 2000 | 4000 | 60° |
| GNL-20003UWC | InGaN | Super White |  | Water Clear |  |  |  | 3.5 | 3000 | 5000 | 60° |