G-NOR ELECTRONICS CO.,LTD.

| # GNL-0805xx (0805 SMD TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter; Unit. DC Forward Current; 30; mA. Reverse Voltage; 5; V. Reverse Current (Vr-5V); 10; µA. Peak Forward Current ,tw ,=1 msec Duty ,=1/20; 150; mA. Operation Temperature; -40; +80; ℃. Storage Temperature; -40; +100; ℃. Solder Dip Temperature (5 seconds,1.6mm from body ); 300; ±5; ℃. |  |
| --- | --- |
| Features: Compatible with automatic placement equipment Compatible with reflow solder process Applications: Automotive and Telecommunication General use for indicators |  |
| Part Number; EMITTED COLOR; Lens Color; Peak Wavelength (nm); Vf (v) Typ.; IV (If=20mA) mcd; View Angle 2θ1/2. Min.; Typ.. GNL-0805GC; GaP; Green; Water Clear; 567; 2.0; 7; 12; 120°. GNL-0805EC; GaP; Orange Red; Water Clear; 635; 2.0; 10; 18; 120°. GNL-0805YC; GaAsP; Yellow; Water Clear; 588; 2.0; 10; 18; 120°. GNL-0805SRC; GaAlAs; Red; Water Clear; 660; 2.0; 9; 15; 120°. GNL-0805UEC; AlGaInP; Super Red; Water Clear; 625; 2.1; 30; 40; 120°. GNL-0805HRC; AlGaInP; Super Red; Water Clear; 640; 2.1; 30; 40; 120°. GNL-0805UEC-TL; AlGaInP; Super Red; Water Clear; 625; 2.1; 120; 200; 120°. GNL-0805UYC; AlGaInP; Super Yellow; Water Clear; 587; 2.1; 30; 40; 120°. GNL-0805UYC-TL; AlGaInP; Super Yellow; Water Clear; 592; 2.1; 100; 150; 120°. GNL-0805PGC; InGaN; Super Pure Green; Water Clear; 525; 3.4; 200; 300; 120°. GNL-0805PGC-TL; InGaN; Super Pure Green; Water Clear; 525; 3.4; 400; 600; 120°. GNL-0805UBC; InGaN; Super Blue; Water Clear; 470; 3.2; 95; 150; 120°. GNL-0805WC; InGaN; Super White; Water Clear; 3.2; 200; 300; 120°. |